## Slide 1: GCCA GNR Concrete Pilot Project - Report on KPIs
July 2020

## Slide 2: Overview
0. Context 03
Process Energy 04
Concrete Transport 11
Circular Economy 24
Local Environment Factors 28
Outcomes of the concrete pilot project 33
Annexes 35

## Slide 3: Concrete pilot project was in the context of extending GNR Data collection generated results at global and regional levels
The objectives of 2020 pilot project are to test the implementation of new GCCA Concrete Test Guidelines and to assess the extension of GNR platform to concrete production.
PwC was in charge of organizing and collecting information on KPIs related to concrete production at site or country level for several territories selected by GCCA. Data collection took place from end of March until end of May 2020.
We would like to thank the following companies who participated to the project: Buzzi Unicem Sp.A and Dyckerhoff, Cementos Argos, CRH plc, HeidelbergCement, Lafarge Holcim, SECIL, Siam City Cement and Votorantim Cimentos.
The total of concrete production collected corresponds to 75 million m3 of concrete. All 9 companies provided quantitative and qualitative feedbacks, and in total between them 46 questionnaires were returned.
KPIs were collected in 29 countries, which represented 6 regions: Europe, North America (USA, Canada, Mexico), South and Central America (Brazil, Colombia, Panama and Dominican Republic), Asia (Turkey, India, Thailand  excluding China), Oceania (Australia) and Africa (Morocco).
The number of companies and the concurring regions in which data were reported are listed below:
Regions | Nb of questionnaires | Nb of reporting companies
Europe | 27 | 6
North America | 9 | 5
South America | 5 | 2
Asia | 3 | 3
Oceania | 1 | 1
Africa | 1 | 1

## Slide 4: Process Energy
1

## Slide 5: Total energy for production is steady in reporting countries The Northern American region with the highest concrete production increases the average
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
kWh/m3 | kWh/m3 | kWh/m3 | kWh/m3 | %
1.2 | 10 | 64 | 11 | 100%
Observations and comments
The Total Energy for concrete production corresponds to the calculated sum of the total electricity energy with the total of non-electricity energy for production, converted in kWh/m3.
The weighted average of energy for production in 2019 is of 10 kWh/m3 at world level, which is increased by a few countries with the highest concrete production.
Around 80% of values lie between 1 kWh/m3 and 6 kWh/m3.
The chart pictures 100% of the world coverage.
Note: Some companies did not provide (or hold) the data split between electricity and non-electricity energy for production, which explains why the coverage is only around 75% for electricity and thermal energy consumption.
World level
Chart: Total energy for production 100% of GNR pilot sample - World (coverage: 75M m3 in 2019)
| 9.1348806580365659E-3 | 1.4625647716349851E-2 | 6.1315708861609579E-2 | 6.5153697319461093E-2 | 7.1454333063328559E-2 | 7.3220509614459278E-2 | 8.015679725639191E-2 | 9.0648184390311276E-2 | 0.10632484001339369 | 0.12399590833063419 | 0.1586531233882312 | 0.1627822272546818 | 0.1971539504199859 | 0.21048197038746752 | 0.2116581319105538 | 0.21373728778826834 | 0.23961688380027177 | 0.25067650172567213 | 0.26168712257207516 | 0.27150862547413029 | 0.27685199186327125 | 0.31003877048802719 | 0.3114338726523378 | 0.35889932504930083 | 0.35909851532223963 | 0.4472962072164588 | 0.44890278320880889 | 0.45864746246376764 | 0.46659741956403034 | 0.47712402588615116 | 0.53605283267392523 | 0.54700371972230288 | 0.54984779732385669 | 0.5952617953548146 | 0.6033693268481175 | 0.60404788055141823 | 0.63179769261509544 | 0.67871577348864232 | 0.69549802144807493 | 0.75520584693113468 | 0.7765603350291993 | 0.91458682509423894 | 0.92238762109712868 | 0.96135167673544997 | 0.97078347886756633 | 1
 | 1.2337 | 1.4327 | 1.7481 | 1.9308 | 2.0049 | 2.3304 | 2.3982 | 2.4369 | 2.516 | 2.5874 | 2.6847 | 2.718 | 2.7971 | 3.0328 | 3.073 | 3.2949 | 3.3352 | 3.3487 | 3.7416 | 3.8654 | 3.9362 | 3.9914 | 4.067 | 4.1532 | 4.2155 | 4.2837 | 4.3836 | 4.438 | 4.4661 | 4.4733 | 4.484 | 4.5595 | 4.7584 | 4.9238 | 5.1008 | 5.3417 | 5.5402 | 5.9206 | 7.6619 | 9.7675 | 16.0775 | 19.8525 | 31.3481 | 32.1624 | 34.452 | 63.9533
Weighted average | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076 | 10.076

## Slide 6: Total energy for production is steady in reporting countries One country in Northern Europe with an average concrete production increases the average
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
kWh/m3 | kWh/m3 | kWh/m3 | kWh/m3 | %
1.8 | 4.4 | 16 | 3 | 100
Observations and comments
The weighted average of energy for production in 2019 is of 4.4 kWh/m3, which is increased by a few countries with the highest concrete production.
Around 80% of values lie between 1 kWh/m3 and 5 kWh/m3.
The chart pictures 100% of the Europe coverage. One company only held the data for total energy for production and not on total Electricity (and non-electricity) energy for production.
Costs of operating in cold weather in Northern Europe may explain the large gap between the maximum value and the rest of the set of values.
Europe level
Chart: Total energy for production 100% of GNR pilot sample - Europe (coverage: 38M m3 in 2019)
| 9.2145413221783087E-2 | 9.5631060148229377E-2 | 0.1163363918400652 | 0.14727513715098617 | 0.18214996601652517 | 0.25054789320413401 | 0.25869690763412218 | 0.32653140081154719 | 0.33063472971720997 | 0.3817095411448444 | 0.40109281932375285 | 0.41163824787632969 | 0.41439155901501201 | 0.50806724967795058 | 0.50846036267800854 | 0.68252337663543283 | 0.68569404304828507 | 0.70492570551855527 | 0.72061538473786657 | 0.74139022344191341 | 0.76300240358188898 | 0.85262943580180095 | 0.86863009678476177 | 0.86996925997817232 | 0.92473504603013523 | 0.9578557388517025 | 1
 | 1.7481 | 2.3304 | 2.4369 | 2.516 | 2.5874 | 2.6847 | 2.718 | 2.7971 | 3.2949 | 3.3352 | 3.8654 | 3.9362 | 4.067 | 4.1532 | 4.2155 | 4.2837 | 4.3836 | 4.438 | 4.4661 | 4.4733 | 4.5595 | 4.9238 | 5.1008 | 5.3417 | 5.5402 | 7.6619 | 16.0775
Weighted average | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567 | 4.3567

## Slide 7: Total energy for production is steady in reporting countries Canada is the country with the highest consumption of energy for production
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
kWh/m3 | kWh/m3 | kWh/m3 | kWh/m3 | %
1.2 | 21.4 | 64 | 19 | 97
Observations and comments
The weighted average of energy for production in 2019 is of 21 kWh/m3, which is increased by a few countries located in Northern America.
The average of total energy for production in North America is twice the average at world level and five times higher than the average in Europe.
Around 90% of values lie between 1 kWh/m3 and 35 kWh/m3.
The chart pictures 97% of coverage in North America. Not all companies did hold the information on non-electricity energy for production.
Costs of operating in cold weather in Northern America may explain the large gap between the maximum value and the rest of the set of values.
North America
Chart: Total energy for production 97% of GNR pilot participants – North America (coverage: 25M m3 in 2019)
| 2.7148379952255469E-2 | 5.9871360080670691E-2 | 0.15850070284100806 | 0.33594918772197829 | 0.74615658243657224 | 0.76934013367762433 | 0.88513923675833517 | 0.91317005155523345 | 1
 | 1.2337 | 3.7416 | 3.9914 | 9.7675 | 19.8525 | 31.3481 | 32.1624 | 34.452 | 63.9533
Weighted average | 21.385 | 21.385 | 21.385 | 21.385 | 21.385 | 21.385 | 21.385 | 21.385 | 21.385 | 21.385 | 21.385

## Slide 8: The use of electricity and other types of energy is scattered Costs of operating in cold-weathered regions may explain the large gap between the maximum value and the rest of the set of values
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
kWh/m3 | kWh/m3 | kWh/m3 | kWh/m3 | %
1.2 | 4.2 | 8.2 | 1.5 | 79
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
MJ/m3 | MJ/m3 | MJ/m3 | MJ/m3 | %
0 | 29 | 210 | 43 | 76
Around 80% of values lie between 2 kWh/m3 and 6 kWh/m3 of total electricity consumption.
Around 85% of values lie between 0 MJ/m3 and 18 MJ/m3 of total non-electricity consumption.
The average value is increased by Northern American sites with the highest concrete production.
World level
Chart: Total non-electricity energy for production 76% of GNR pilot sample - World (coverage: 57M m3 in 2019)
| 5.4554226914203937E-3 | 1.2709891499194612E-2 | 2.103436875120808E-2 | 9.8891831320852067E-2 | 0.11350393422262114 | 0.12557305063070701 | 0.24210092332484448 | 0.24443441745474043 | 0.24718142371109653 | 0.26789361346893437 | 0.27296441091060075 | 0.31875394868000928 | 0.32791825701903538 | 0.37333059939743279 | 0.38039032063252737 | 0.3933666107740928 | 0.40783505710703888 | 0.45168183621949265 | 0.45352506231653245 | 0.51352659373336673 | 0.53569950565133018 | 0.71806179787557589 | 0.74627560956493633 | 0.82516232119315525 | 0.88715106531633636 | 0.93863085370484844 | 0.94893736109767113 | 0.96139877380046324 | 1
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.027438 | 0.058731 | 0.68073 | 2.4445 | 3.3892 | 3.5477 | 4.2064 | 4.3104 | 5.2515 | 11.4702 | 14.3352 | 14.6087 | 15.8553 | 16.2705 | 26.3886 | 77.853 | 101.5309 | 210
Weighted average | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258 | 29.1258
Chart: Total electricity energy for production 79% of GNR pilot sample - World (coverage: 59M m3 in 2019)
| 1.1633240970551987E-2 | 7.1383265202957541E-2 | 7.8375739291421068E-2 | 8.3263405178233038E-2 | 9.1287244418168725E-2 | 9.3536464543202982E-2 | 0.10236980441926086 | 0.12233397464793629 | 0.1661062529210309 | 0.21024210419551562 | 0.21550050461354389 | 0.25776375984704253 | 0.25954041794072935 | 0.27204807011810783 | 0.28902126043621407 | 0.29051909833148165 | 0.29732385814453272 | 0.29997165642961632 | 0.31405604408444887 | 0.37189062368188619 | 0.38583654291652841 | 0.39985853294974261 | 0.51217800829497206 | 0.53355014678786794 | 0.6085957916224467 | 0.61221771524864288 | 0.6882554378718736 | 0.71545030939206322 | 0.89122659803284254 | 0.92843374319196481 | 0.97805434201520258 | 0.99006571152258049 | 1
 | 1.2337 | 1.4011 | 1.4327 | 1.9308 | 2.0049 | 2.3304 | 2.3818 | 2.516 | 2.608 | 2.6771 | 2.718 | 2.8229 | 2.8697 | 2.9239 | 3.0328 | 3.073 | 3.2572 | 3.2949 | 3.3487 | 3.465 | 3.5741 | 3.7416 | 4.2837 | 4.4757 | 4.484 | 4.7584 | 5.3633 | 5.4729 | 5.5173 | 5.62 | 5.7738 | 6.249 | 8.16
Average | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462 | 4.0462

## Slide 9: The use of electricity and other types of energy is scattered Not all companies held the data split between electricity and non-electricity energy for production
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
kWh/m3 | kWh/m3 | kWh/m3 | kWh/m3 | %
2.3 | 3.6 | 5.5 | 0.9 | 58
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
MJ/m3 | MJ/m3 | MJ/m3 | MJ/m3 | %
0 | 5.7 | 53 | 13 | 58
Around 80% of values lie between 2 kWh/m3 and 4 kWh/m3 of total electricity consumption.
Around 70% of values lie between 0 MJ/m3 and 4 MJ/m3 of total non-electricity consumption.
Europe level
Chart: Total electricity energy for production 58% of GNR pilot sample - Europe (coverage: 22M m3 in 2019)
| 6.0498071435915648E-3 | 5.9748143878631546E-2 | 0.17748399322499622 | 0.29619775776807528 | 0.31034146387259354 | 0.31512020416007092 | 0.3487624798315595 | 0.36706548364573444 | 0.37418736060281726 | 0.52974708057013764 | 0.56725791415669213 | 0.8693675906374122 | 0.92685298954925921 | 1
 | 2.3304 | 2.516 | 2.608 | 2.6771 | 2.718 | 2.8697 | 2.9239 | 3.2572 | 3.2949 | 3.465 | 3.5741 | 4.2837 | 4.4757 | 5.4729
Weighted average | 3.6325 | 3.6325 | 3.6325 | 3.6325 | 3.6325 | 3.6325 | 3.6325 | 3.6325 | 3.6325 | 3.6325 | 3.6325 | 3.6325 | 3.6325 | 3.6325 | 3.6325 | 3.6325
Chart: Total non-electricity energy for production 58% of GNR pilot sample - Europe (coverage: 22M m3 in 2019)
| 1.4143706104518219E-2 | 0.31625338258523827 | 0.32230318972882982 | 0.32942506668591259 | 0.38312340342095258 | 0.50183716796403166 | 0.61957301731039638 | 0.63787602112457131 | 0.67151829679606001 | 0.70902913038261439 | 0.71380787067009177 | 0.86936759063741209 | 0.92685298954925921 | 1
 | 0 | 0 | 0 | 0 | 0 | 0.027438 | 0.68073 | 2.4445 | 3.3892 | 3.5477 | 4.3104 | 5.2515 | 11.4702 | 52.5913
Weighted average | 5.719 | 5.719 | 5.719 | 5.719 | 5.719 | 5.719 | 5.719 | 5.719 | 5.719 | 5.719 | 5.719 | 5.719 | 5.719 | 5.719 | 5.719 | 5.719

## Slide 10: The use of energy is high in Northern America, especially in Canada One company did not hold the information on the energy consumption of the auxiliary diesel plants
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
kWh/m3 | kWh/m3 | kWh/m3 | kWh/m3 | %
1.2 | 5.2 | 8.6 | 2,01 | 100
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
MJ/m3 | MJ/m3 | MJ/m3 | MJ/m3 | %
0 | 60.3 | 210 | 68 | 97
Around 80% of values lie between 2 kWh/m3 and 6 kWh/m3 of total electricity consumption.
Around 60% of values lie between 4 MJ/m3 and 27 MJ/m3 of total non-electricity consumption.
North America
Chart: Total electricity energy for production 100% of GNR pilot sample - North America (coverage: 25M m3 in 2019)
| 2.7148379952255469E-2 | 0.12577772271259283 | 0.15850070284100806 | 0.33594918772197829 | 0.74615658243657224 | 0.83298653088133878 | 0.94878563396204962 | 0.97681644875894791 | 1
 | 1.2337 | 2.8229 | 3.7416 | 5.3633 | 5.5173 | 5.62 | 5.7738 | 6.249 | 8.16
Weighted average | 5.1764 | 5.1764 | 5.1764 | 5.1764 | 5.1764 | 5.1764 | 5.1764 | 5.1764 | 5.1764 | 5.1764 | 5.1764
Chart: Total non-electricity energy for production 97% of GNR pilot sample - North America (coverage: 25M m3 in 2019)
| 2.806680960523561E-2 | 0.13003278288291292 | 0.55411749314415004 | 0.73756906000193412 | 0.85728564656581663 | 0.88125349731050806 | 0.91023259452985439 | 1
 | 0 | 4.2064 | 14.3352 | 15.8553 | 26.3886 | 77.853 | 101.5309 | 210
Weighted average | 60.3271 | 60.3271 | 60.3271 | 60.3271 | 60.3271 | 60.3271 | 60.3271 | 60.3271 | 60.3271 | 60.3271

## Slide 11: Concrete Transport
2

## Slide 12: The average distribution distance is patchily deployed The distribution distance varies according to GNR pilot participants
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
km | km | km | km | %
5 | 16 | 61 | 9 | 100
Observations and comments
The weighted average of journey distance in 2019 is of 16 km at world level for a single trip.
Around 80% of values lie between 10 km and 30 km.
The chart pictures 100% of the world coverage.
Distribution distances can vary according to regions and presumably according to the distribution network of sites participating to the pilot project.
World level
Chart: Average distribution distance 100% of GNR pilot sample – World (coverage: 75M m3 in 2019)
| 1.1059617925400373E-2 | 4.5431341090704444E-2 | 0.13362903298492362 | 0.16828624804252065 | 0.17639377953582347 | 0.18740440038222655 | 0.19722590328428172 | 0.2140081512437142 | 0.21935151763285513 | 0.2485680387652888 | 0.25269714263173942 | 0.26064709973200206 | 0.26844789573489181 | 0.26962405725797806 | 0.31631411840323781 | 0.37524292519101193 | 0.37592147889431266 | 0.37612066916725151 | 0.42358612156421455 | 0.4333308008191733 | 0.43472590298348385 | 0.44021667004179715 | 0.44964847217391363 | 0.47739828423759079 | 0.48653316489562737 | 0.49037115335347886 | 0.53578515138443683 | 0.58270323225798371 | 0.60858282826998711 | 0.62625389658722752 | 0.68596172207028738 | 0.70731621016835189 | 0.72299286579143429 | 0.73394375283981195 | 0.73602290871752651 | 0.74232354446139392 | 0.75565156442887549 | 0.79461562006719677 | 0.79622219605954692 | 0.80674880238166768 | 0.81724018951558708 | 0.85042696814034302 | 0.85219314469147378 | 0.85912943233340644 | 0.99715592239844608 | 1
 | 5.2213 | 6.83 | 6.95 | 7.5 | 8.3682 | 8.6237 | 9.2477 | 9.4367 | 9.4367 | 10 | 10.0775 | 10.8538 | 11.3191 | 11.3496 | 11.5705 | 11.7 | 11.7607 | 12.1175 | 12.2608 | 12.415 | 12.7821 | 12.9452 | 13.0357 | 13.3391 | 13.3969 | 14.3287 | 14.438 | 14.79 | 16.6817 | 16.8545 | 16.945 | 18.0906 | 18.3274 | 19.6039 | 19.7212 | 19.732 | 20.919 | 21.3734 | 21.3878 | 21.53 | 21.6 | 22.9786 | 26 | 28.5204 | 29.3026 | 60.7519
Weighted average | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185 | 15.8185

## Slide 13: The average distribution distance is patchily deployed The distribution distance varies according to GNR pilot participants
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
km | km | km | km | %
6.8 | 12 | 26 | 5 | 100%
Observations and comments
The weighted average of journey distance in 2019 is of 12 km at European level for a single trip.
Around 75% of values lie between 10 km and 30 km.
The chart pictures 100% of Europe coverage.
There is no identified common pattern for the average distribution distance in reporting sites. The data on distribution distances do not vary according to the width of European reporting countries nor the size of concrete production.
One assumption that can be raised is that the average distance varies according to the distribution network of sites participating to the pilot project.
Europe level
Chart: Average distribution distance 100% of GNR pilot sample - Europe (coverage: 38M m3 in 2019)
| 6.7834493177425015E-2 | 0.24189750713484928 | 0.31029543432245815 | 0.32629609530541892 | 0.34567937348432737 | 0.37880006630589447 | 0.38934549485847131 | 0.39749450928845947 | 0.41318418850777078 | 0.50532960172955388 | 0.50666876492296442 | 0.50706187792302249 | 0.60073756858596106 | 0.61996923105623114 | 0.62272254219491352 | 0.67748832824687644 | 0.76711536046678841 | 0.81819017189442289 | 0.85306500075996183 | 0.89520926190825945 | 0.92614800721918045 | 0.94776018735915601 | 0.95186351626481869 | 0.95503418267767093 | 0.97580902138171788 | 0.99651435307355363 | 1
 | 6.83 | 6.95 | 7.5 | 8.3682 | 9.2477 | 9.4367 | 9.4367 | 10.0775 | 10.8538 | 11.5705 | 11.7607 | 12.1175 | 12.2608 | 12.415 | 12.7821 | 13.3391 | 14.438 | 16.6817 | 16.8545 | 18.0906 | 18.3274 | 19.6039 | 19.7212 | 21.3878 | 21.53 | 21.6 | 26
Weighted average | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224 | 12.0224

## Slide 14: The average distribution distance is homogeneous in America The distribution distance varies according to GNR pilot participants
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
km | km | km | km | %
8.6 | 23 | 29 | 7 | 100
Observations and comments
The weighted average of journey distance in 2019 is of 23 km for a single trip in North America.
Around 70% of values lie between 8 km and 20 km.
The chart pictures 100% of the coverage in North America.
The average distribution distance in North America is almost twice the average of Europe, with respectively 23 km and 12 km as weighted averages for a single trip.
This can be explain by the width of countries in North America, which is higher than the one of European countries.
North America
Chart: Average distribution distance 100% of GNR pilot sample - North America (coverage: 25M m3 in 2019)
| 3.2722980128415222E-2 | 0.11955292857318181 | 0.14273647981423393 | 0.17076729461113219 | 0.19791567456338766 | 0.37536415944435791 | 0.49116326252506876 | 0.58979260528540611 | 1
 | 8.6237 | 10 | 11.3191 | 13.0357 | 13.3969 | 16.945 | 21.3734 | 22.9786 | 29.3026
Weighted average | 23.1612 | 23.1612 | 23.1612 | 23.1612 | 23.1612 | 23.1612 | 23.1612 | 23.1612 | 23.1612 | 23.1612 | 23.1612

## Slide 15: The average concrete volume transported is balanced The data correspond to the average shipping volume of a concrete truck
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
m3/delivery | m3/delivery | m3/delivery | m3/delivery | %
4.5 | 6.6 | 10 | 1 | 100
Observations and comments
The weighted average of the concrete volume transported in 2019 is of 7 m3/delivery at world level.
Around 80% of values lie between 4.5 and 8 m3/delivery.
The standard deviation of average concrete volume transported is low, as figures vary from 4.5 to 10 m3/delivery.
Most of the pilots participants data are close to the average truck capacity of 8 m3, which means that most of the trucks circulating in reporting countries are optimally loaded.
The chart pictures 100% of the world coverage.
World level
Chart: Average concrete volume transported 100% of GNR pilot sample - World (coverage: 75M m3 in 2019)
| 3.8379884578515129E-3 | 1.4364594779972335E-2 | 1.8493698646422946E-2 | 1.8692888919361751E-2 | 4.0047377017426306E-2 | 9.8976183805200388E-2 | 0.23700267387024015 | 0.23876885042137089 | 0.28568693129491779 | 0.29511873342703426 | 0.29796281102858807 | 0.31129083099606975 | 0.3567048290270276 | 0.37348707698646005 | 0.37556623286417457 | 0.40144582887617797 | 0.44891128127314101 | 0.48328300443844507 | 0.48445916596153132 | 0.50213023427877179 | 0.51008019137903449 | 0.52113980930443493 | 0.58084763478749468 | 0.59066913768954987 | 0.59206423985386047 | 0.62525101847861653 | 0.63499569773357523 | 0.64413057839161181 | 0.73232827028583103 | 0.73862890602969844 | 0.77759296166801972 | 0.78293632805716062 | 0.79394694890356365 | 0.84063701004882341 | 0.84843780605171315 | 0.84911635975501387 | 0.87686617181869109 | 0.88235693887700439 | 0.91157346000943806 | 0.92725011563252047 | 0.96190733069011747 | 0.97001486218342026 | 0.9716214381757704 | 0.97855772581770306 | 0.98950861286608061 | 1
 | 4.5 | 4.5742 | 4.6413 | 4.9507 | 4.9879 | 5.4 | 5.5208 | 5.5747 | 5.66 | 5.91 | 6.1963 | 6.4587 | 6.4629 | 6.4645 | 6.4837 | 6.504 | 6.536 | 6.54 | 6.5595 | 6.5809 | 6.6418 | 6.6571 | 6.7 | 6.701 | 6.7128 | 6.7746 | 6.7952 | 6.8427 | 6.95 | 7.001 | 7.0673 | 7.0839 | 7.2095 | 7.3139 | 7.5968 | 7.6901 | 7.9602 | 8 | 8 | 8.0395 | 8.0477 | 8.3853 | 8.3943 | 8.85 | 9.3264 | 10.0601
Weighted average | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149 | 6.6149

## Slide 16: The average concrete volume transported is balanced The data correspond to the average shipping volume of a concrete truck
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
m3/delivery | m3/delivery | m3/delivery | m3/delivery | %
4.6 | 7 | 10 | 1 | 100
Observations and comments
The weighted average of the concrete volume transported in 2019 is of 7 m3/delivery at European level.
Around 80% of values lie between 4.5 and 8 m3/delivery.
The standard deviation of average concrete volume transported is low, as figures vary from 4.5 to 10 m3/delivery.
Most of the pilots participants data are close to the average truck capacity of 8 m3, which means that most of the trucks circulating in reporting countries are optimally loaded.
The chart pictures 100% of Europe coverage.
Europe level
Chart: Average concrete volume transported 100% of GNR pilot sample - Europe (coverage: 38M m3 in 2019)
| 2.077483870404688E-2 | 2.8923853134035102E-2 | 2.9316966134093136E-2 | 7.1461227282390682E-2 | 7.4946874208836972E-2 | 0.16457390642874897 | 0.19769459925031607 | 0.20179792815597883 | 0.25287273958361323 | 0.34654843024655174 | 0.41438292342397676 | 0.44925775228951575 | 0.46494743150882706 | 0.48433070968773551 | 0.48708402082641783 | 0.50631568329668797 | 0.68037869725411226 | 0.69092412580668905 | 0.78306953902847221 | 0.78440870222188275 | 0.83917448827384566 | 0.87011323358476667 | 0.93851116077237562 | 0.95451182175533633 | 0.95768248816818857 | 0.97929466830816414 | 1
 | 4.5742 | 4.6413 | 4.9507 | 4.9879 | 5.5747 | 6.4629 | 6.4645 | 6.4837 | 6.504 | 6.536 | 6.54 | 6.5809 | 6.6418 | 6.701 | 6.7128 | 6.7952 | 6.95 | 7.0839 | 7.3139 | 7.6901 | 7.9602 | 8.0395 | 8.0477 | 8.3853 | 8.3943 | 9.3264 | 10.0601
Weighted average | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597 | 6.9597

## Slide 17: The average concrete volume transported is balanced The data correspond to the average shipping volume of a concrete truck
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
m3/delivery | m3/delivery | m3/delivery | m3/delivery | %
5.5 | 6.4 | 8 | 1 | > 60
Observations and comments
The weighted average of the concrete volume transported in 2019 is of 6.4 m3/delivery at European level.
Around 80% of values lie between 5.5 and 7 m3/delivery.
Most of the pilots participants data are around to the average truck capacity of 8 m3, which means that most of the trucks circulating in reporting countries are almost optimally loaded.
The chart pictures > 60% of the coverage in North America.
Note: Coverage is not provided for confidentiality reasons.
North America
Chart: Average concrete volume transported > 60% of GNR pilot sample - North America (coverage: > 15M m3 in 2019)
| 0.41020739471459389 | 0.43823820951149217 | 0.61568669439246237 | 0.71431603715279979 | 0.74146441710505528 | 0.85726352018576613 | 0.88044707142681822 | 0.91317005155523345 | 1
 | 5.5208 | 5.91 | 6.7 | 6.7746 | 6.8427 | 7.0673 | 6.83 | 7.2095 | 8
Weighted average | 6.3966 | 6.3966 | 6.3966 | 6.3966 | 6.3966 | 6.3966 | 6.3966 | 6.3966 | 6.3966 | 6.3966 | 6.3966

## Slide 18: Fuel consumption patterns can be observed at a country scale The reported type of fuel of all GNR pilot participants is diesel.
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
km/l | km/l | km/l | km/l | %
0.1 | 1.15 | 2,6 | 1 | 79
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
l/km/m3 | l/km/m3 | l/km/m3 | l/km/m3 | %
0.5 | 4.8 | 13.8 | 3 | 80
Around 75% of values lie between 0 and 2 km/l.
Almost 24% of the sample data are based on the estimated value of 2.6 km/l average fuel consumption, that is used for several countries by one contributor.
Around 80% of values lie between 1 and 5 l/km/m3.
World level
Chart: Distance per liter* 79% of GNR pilot sample - World (coverage: 59M m3 in 2019)
| 5.8738396247625502E-2 | 7.2590299508070263E-2 | 8.9357604986865569E-2 | 9.0837274104867249E-2 | 9.6031890113199528E-2 | 0.10584567564753591 | 0.27948979748506686 | 0.31624561988407535 | 0.31800072711082 | 0.33191427110958305 | 0.37515559154212857 | 0.3870212631085429 | 0.39722093699549976 | 0.43213156715557394 | 0.43415271887235984 | 0.46101771653571511 | 0.49357552280099681 | 0.49382611397379805 | 0.54284481481417168 | 0.61796019967941751 | 0.62153818936333172 | 0.63303031909297969 | 0.64303175663348855 | 0.70205701292849632 | 0.70998352297918654 | 0.73221459716235482 | 0.73912225252333641 | 0.75232093420298041 | 0.76104712564513299 | 0.78076913044100094 | 0.79302841683608627 | 0.79388207081130324 | 0.79871044929917301 | 0.85584349530723369 | 0.89944397859978953 | 0.91322073380063162 | 0.95497133564667469 | 0.95719327272619192 | 0.96391549078637262 | 0.97627142511280884 | 0.97888710559833714 | 1
 | 0.11458 | 0.18817 | 0.25589 | 0.3344 | 0.38413 | 0.39755 | 0.42375 | 0.5 | 0.5 | 0.51897 | 0.543 | 0.56535 | 0.59908 | 0.62295 | 0.66955 | 0.74578 | 0.78699 | 0.78756 | 0.81311 | 1.1 | 1.2039 | 1.2254 | 1.3177 | 1.5 | 1.5099 | 1.5183 | 1.53 | 1.533 | 1.5961 | 1.7118 | 1.8399 | 1.8399 | 2.3 | 2.6 | 2.6 | 2.6 | 2.6 | 2.6 | 2.6 | 2.6 | 2.6 | 2.6
Weighted average | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507 | 1.1507
Chart: Fuel consumption 79% of GNR pilot sample - World (coverage: 59M m3 in 2019)
| 4.3600483292555843E-2 | 5.3601920833064684E-2 | 6.5957855159500894E-2 | 7.9734610360343017E-2 | 0.13686765636840365 | 0.14912694276348898 | 0.15584916082366965 | 0.16275681618465129 | 0.18386971058631416 | 0.18472336456153113 | 0.22647396640757414 | 0.24619597120344214 | 0.25102434969131188 | 0.26422303137095582 | 0.27813657536971892 | 0.28962870509936689 | 0.29982837898632375 | 0.32205945316949203 | 0.38108470946449979 | 0.38330664654401708 | 0.39123315659470725 | 0.43447447702725278 | 0.44320066846940537 | 0.51831605333465114 | 0.52093173382017932 | 0.55768755621918775 | 0.59259818637926198 | 0.59284877755206322 | 0.62540658381734493 | 0.67442528465771867 | 0.68423907019205499 | 0.68626022190884095 | 0.68801532913558561 | 0.69988100070199999 | 0.72674599836535525 | 0.72822566748335693 | 0.7334202834916892 | 0.74727218675213403 | 0.75085017643604823 | 0.92449429827357932 | 0.94126160375237455 | 1
 | 0.35844 | 0.51236 | 0.53078 | 0.80845 | 0.85922 | 0.99301 | 1.0247 | 1.0576 | 1.1165 | 1.1699 | 1.3046 | 1.3317 | 1.3844 | 1.4005 | 1.5113 | 1.5978 | 1.6658 | 1.6868 | 1.742 | 1.7938 | 1.8666 | 1.9233 | 2.019 | 2.2992 | 2.3398 | 2.5 | 2.69 | 3.1079 | 3.2591 | 3.7194 | 3.7479 | 3.8054 | 3.8083 | 4.3192 | 4.8632 | 5.1742 | 5.6524 | 6.3567 | 8.1439 | 12.5255 | 12.6572 | 13.8064
Weighted average | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004 | 4.8004
*corresponds to Concrete Transport KPI #4 Average fuel consumption

## Slide 19: Fuel consumption patterns can be observed at a country scale The reported type of fuel of all GNR pilot participants is diesel.
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
km/l | km/l | km/l | km/l | %
0.1 | 1.4 | 3 | 1 | 70
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
l/km/m3 | l/km/m3 | l/km/m3 | l/km/m3 | %
0.4 | 3.3 | 13.8 | 3 | 70
Around 70% of values lie between 0 and 2 km/l.
Almost 30% of the sample data are based on the estimated value of 2.6 km/l average fuel consumption, that is used for several countries by one contributor.
Around 70% of values lie between 1 and 5 l/km/m3.
Europe level
Chart: Fuel consumption 70% of GNR pilot sample - Europe (coverage: 27M m3 in 2019)
| 9.4691636853229774E-2 | 0.11641278350294634 | 0.14324743206339052 | 0.17316782289347837 | 0.29724951273653177 | 0.32387426108195572 | 0.33847359079882444 | 0.39932868969184987 | 0.40118265749484811 | 0.44401495601817292 | 0.47267988535311006 | 0.4948315621876187 | 0.543113063777515 | 0.54793867219182124 | 0.64185027826229424 | 0.64753101957421466 | 0.72335001202101545 | 0.72389424654645185 | 0.79460337027160644 | 0.79899291254128679 | 0.80280465873314055 | 0.86115012673476798 | 0.87243180655818764 | 1
 | 0.35844 | 0.51236 | 0.53078 | 0.80845 | 0.85922 | 0.99301 | 1.0247 | 1.1165 | 1.1699 | 1.3317 | 1.4005 | 1.6658 | 1.6868 | 1.7938 | 1.9233 | 2.3398 | 2.69 | 3.1079 | 3.2591 | 3.8054 | 3.8083 | 4.8632 | 5.6524 | 13.8064
Weighted average | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301 | 3.3301
Chart: Distance per liter* 70% of GNR pilot sample - Europe (coverage: 27M m3 in 2019)
| 0.13014873987846384 | 0.1416586341014317 | 0.14554748719420976 | 0.24135880865507064 | 0.26395858645564979 | 0.34131130314444463 | 0.34578964041354415 | 0.40531536491551179 | 0.47745484657193965 | 0.47801009028726438 | 0.50017062881104146 | 0.54942880533473171 | 0.57867359066085589 | 0.62237233349404997 | 0.64953566749798186 | 0.65142713877170122 | 0.77801884740501237 | 0.87462597870454206 | 0.90515162195575971 | 0.92004627801740069 | 0.947423758257538 | 0.95321941392510234 | 1
 | 0.11458 | 0.38413 | 0.5 | 0.543 | 0.59908 | 0.62295 | 0.66955 | 0.74578 | 0.78699 | 0.78756 | 1.3177 | 1.5183 | 1.533 | 1.7118 | 1.8399 | 1.8399 | 2.6 | 2.6 | 2.6 | 2.6 | 2.6 | 2.6 | 2.6
Weighted average | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288 | 1.4288
*corresponds to Concrete Transport KPI #4 Average fuel consumption

## Slide 20: Fuel consumption patterns can be observed at a country scale The reported type of fuel of all GNR pilot participants is diesel.
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
km/l | km/l | km/l | km/l | %
0.2 | 0.8 | 3 | 0.7 | 100
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
l/km/m3 | l/km/m3 | l/km/m3 | l/km/m3 | %
1.3 | 7.5 | 12.5 | 3 | 100
Around 70% of values lie between 0 and 1 km/l.
The chart picture 100% of coverage in North America.
The weighted average is the lowest in comparison to global level and European level with 0.8 km/l.
Around 80% of values lie between 1 and 5 l/km/m3.
The chart picture 100% of coverage in North America.
Therefore, North America consumes more diesel fuel for less distance travelled.
North America
Chart: Distance per liter* 100% of GNR pilot sample - North America (coverage: 25M m3 in 2019)
| 3.2722980128415222E-2 | 5.5906531369467341E-2 | 0.46611392608406127 | 0.55294387452882787 | 0.58097468932572605 | 0.69677379240643689 | 0.8742222772874072 | 0.9013706572396627 | 1
 | 0.18817 | 0.39755 | 0.42375 | 0.5 | 0.56535 | 0.81311 | 1.1 | 1.2254 | 2.6
Weighted average | 0.82813 | 0.82813 | 0.82813 | 0.82813 | 0.82813 | 0.82813 | 0.82813 | 0.82813 | 0.82813 | 0.82813 | 0.82813
Chart: Fuel consumption 100% of GNR pilot sample - North America (coverage: 25M m3 in 2019)
| 9.8629342760337357E-2 | 0.12577772271259283 | 0.30322620759356306 | 0.39005615603832966 | 0.5058552591190405 | 0.52903881036009259 | 0.55706962515699088 | 0.58979260528540611 | 1
 | 1.3046 | 1.5978 | 2.2992 | 2.5 | 3.7194 | 3.7479 | 4.3192 | 6.3567 | 12.5255
Weighted average | 7.4552 | 7.4552 | 7.4552 | 7.4552 | 7.4552 | 7.4552 | 7.4552 | 7.4552 | 7.4552 | 7.4552 | 7.4552
*corresponds to Concrete Transport KPI #4 Average fuel consumption

## Slide 21: CO2 emissions from transport vary according to regions The reported data broadly come from company-owned trucks.
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
kg CO2/m3 | kg CO2/m3 | kg CO2/m3 | kg CO2/m3 | %
0.96 | 11 | 71 | 12 | 79
Observations and comments
The weighted average is of 11 kg CO2/m3 of concrete from transport at world level.
More than 80% of values lie between 2 and 15 kg CO2/m3.
The maximum value of 71 kg CO2/m3 corresponds to one country isolated from other reporting countries.
The chart pictures 80% of the world coverage. The remaining 20% corresponds to missing data on average fuel consumption, coming for example from contractors and customers, which would be too sensitive to start collecting.
World level
Chart: Gross CO2 emissions from transport 79% of GNR pilot sample - World (coverage: 75M m3 in 2019)
| 4.3600483292555843E-2 | 5.0322701352736511E-2 | 6.2678635679172715E-2 | 7.6455390880014837E-2 | 7.7309044855231809E-2 | 0.13444209086329245 | 0.14670137725837773 | 0.1536090326193594 | 0.17472192702102224 | 0.1773376075065505 | 0.18733904504705934 | 0.22908964689310235 | 0.24881165168897035 | 0.25364003017684011 | 0.26683871185648406 | 0.2807522558552471 | 0.29224438558489507 | 0.30244405947185193 | 0.3614693157668597 | 0.36369125284637699 | 0.38592232702954532 | 0.42916364746209085 | 0.43788983890424343 | 0.44581634895493361 | 0.52093173382017932 | 0.55768755621918775 | 0.59259818637926198 | 0.59284877755206322 | 0.62540658381734493 | 0.63522036935168136 | 0.63724152106846732 | 0.63899662829521198 | 0.68801532913558561 | 0.69320994514391798 | 0.70507561671033225 | 0.73194061437368763 | 0.7334202834916892 | 0.90706440532922028 | 0.91064239501313449 | 0.92449429827357932 | 0.98323269452120476 | 1
 | 0.96062 | 1.3731 | 1.4225 | 2.1666 | 2.2276 | 2.3027 | 2.6613 | 2.8344 | 2.9921 | 3.1353 | 3.3237 | 3.4962 | 3.5367 | 3.7102 | 3.7535 | 4.0805 | 4.314 | 4.4643 | 4.7035 | 4.8074 | 5.0311 | 5.1929 | 5.4324 | 5.4514 | 6.2078 | 6.75 | 7.2091 | 8.329 | 8.6927 | 9.7368 | 10.1985 | 10.1997 | 10.3215 | 10.9281 | 11.5753 | 13.0333 | 14.171 | 16.4898 | 22.1063 | 24.3324 | 37.0011 | 70.9408
Weighted average | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638 | 10.638

## Slide 22: CO2 emissions from transport vary according to countries The reported data broadly come from company-owned trucks.
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
kg CO2/m3 | kg CO2/m3 | kg CO2/m3 | kg CO2/m3 | %
0.96 | 9 | 37 | 7 | 70
Observations and comments
The weighted average is of 9 kg CO2/m3 of concrete from transport at European level.
Around 80% of values lie between 2 and 11 kg CO2/m3.
The maximum value of 37 kg CO2/m3, corresponding to one country isolated from other reporting countries, increases the average of 3 kg CO2/m3 .
The chart pictures 70% of Europe coverage. The remaining 30% corresponds to missing data on average fuel consumption, coming for example from contractors and customers, which would be too sensitive to start collecting.
Europe level
Chart: Gross CO2 emissions from transport 70% of GNR pilot sample - Europe (coverage: 25M m3 in 2019)
| 0.10415071467547632 | 0.12020842234982557 | 0.14972367753511151 | 0.18263292054622679 | 0.18467208765838558 | 0.3211487302084084 | 0.35043311751421319 | 0.40086657317218022 | 0.40711478354412756 | 0.43100573128057118 | 0.4781166974719373 | 0.50964506656099595 | 0.53400955164377306 | 0.53931720691086893 | 0.59242171606606508 | 0.69571447996370339 | 0.69631307997378789 | 0.77408558465090338 | 0.77891361360549882 | 0.78310612841711236 | 0.79551477458055631 | 0.85968857484829719 | 1
 | 0.96062 | 1.3731 | 1.4225 | 2.1666 | 2.2276 | 2.3027 | 2.6613 | 2.9921 | 3.1353 | 3.3237 | 3.5367 | 3.7535 | 4.4643 | 4.8074 | 5.0311 | 5.1929 | 8.329 | 8.6927 | 10.1985 | 10.1997 | 10.9281 | 13.0333 | 37.0011
Weighted average | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005 | 8.9005

## Slide 23: CO2 emissions from transport vary according to countries The reported data broadly come from company-owned trucks.
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
kg CO2/m3 | kg CO2/m3 | kg CO2/m3 | kg CO2/m3 | %
3.5 | 13 | 24 | 5 | 100
Observations and comments
The weighted average is of 13 kg CO2/m3 of concrete from transport at European level.
Around 80% of values lie between 3 and 11 kg CO2/m3.
The chart pictures 100% of coverage in North America.
The United States is the country with the largest amount of CO2 emissions from transport of concrete.
North America
Chart: Gross CO2 emissions from transport 100% of GNR pilot sample - Europe (coverage: 25M m3 in 2019)
| 9.8629342760337371E-2 | 0.12577772271259285 | 0.30322620759356311 | 0.39005615603832972 | 0.41323970727938181 | 0.5290388103600927 | 0.55706962515699099 | 0.96727701987158488 | 1
 | 3.4962 | 4.314 | 6.2078 | 6.75 | 9.7368 | 10.3215 | 11.5753 | 16.4898 | 24.3324
Weighted average | 13.2376 | 13.2376 | 13.2376 | 13.2376 | 13.2376 | 13.2376 | 13.2376 | 13.2376 | 13.2376 | 13.2376 | 13.2376

## Slide 24: Circular Economy
3

## Slide 25: Wasted and returned concrete are not consistently monitored Procedures for returned and scrap concrete are in place in 70% of cases.
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
% | % | % | % | %
0 | 0.5 | 4 | 1 | 56
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
% | % | % | % | %
0% | 53% | 100% | 30 | 51
Around 80% of values lie between 0% and 1% of wasted concrete at world level.
The chart pictures 56% of the world coverage due to missing data.
Around 60% of values lie between 40% and 80% of returned concrete recovered at world level.
The chart pictures 51% of the world coverage due to missing data.
World level
Chart: Wasted concrete 56% of GNR pilot sample – World (coverage: 42M m3 in 2019)
| 9.8306480559964514E-3 | 6.1538999911615877E-2 | 0.17687555520024956 | 0.18059806782376756 | 0.18799079937960225 | 0.20557518010194012 | 0.23364260355824001 | 0.31764455367416888 | 0.33744565073469496 | 0.49535445639975029 | 0.51170951131811959 | 0.61861017060289503 | 0.62110795610969982 | 0.68315809959855478 | 0.76446714562375762 | 0.77403388809307327 | 0.80408075978249538 | 0.82368718550230013 | 0.82684934115278108 | 0.88626682095249087 | 0.89754745476361086 | 0.90996615726889329 | 0.9622753034452326 | 0.97624181836866675 | 0.98311333802546763 | 1
 | 0 | 0 | 0.00015968 | 0.00042923 | 0.00068792 | 0.00087255 | 0.0013197 | 0.0014872 | 0.0017521 | 0.002428 | 0.0024822 | 0.0026083 | 0.0036008 | 0.0046306 | 0.006 | 0.0060854 | 0.0065532 | 0.0099629 | 0.01 | 0.012561 | 0.015035 | 0.019345 | 0.021485 | 0.023875 | 0.04
Weighted average | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434 | 0.0048434
Chart: Returned Concrete Recovered 51% of GNR pilot sample – World (coverage: 38M m3 in 2019)
| 1.3498787745898251E-2 | 0.12969686149538742 | 0.1331340376357433 | 0.14060319033502636 | 0.16654100057324192 | 0.16882994180155148 | 0.17436483335422387 | 0.18954605058856575 | 0.20732354504273018 | 0.22567888173220987 | 0.29312567951179286 | 0.34998428137484733 | 0.37129592638243064 | 0.39281917377822556 | 0.48119986843202073 | 0.48923556411699015 | 0.51066345774378108 | 0.52292519614928201 | 0.52697146489313196 | 0.54608520265381488 | 0.54880022673759477 | 0.58146034909669186 | 0.59185913479576413 | 0.68316694206259676 | 0.85480946671234914 | 0.88531798333473211 | 1
 | 0 | 0 | 0 | 0 | 0 | 0 | 0.12271 | 0.17331 | 0.18436 | 0.2 | 0.39855 | 0.40559 | 0.44328 | 0.46388 | 0.50582 | 0.51864 | 0.55219 | 0.55797 | 0.65278 | 0.66 | 0.6836 | 0.7 | 0.7 | 0.74156 | 0.74367 | 0.93526 | 1
Weighted average | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311 | 0.53311

## Slide 26: Wasted and returned concrete are not consistently monitored Procedures for returned and scrap concrete are in place in 70% of cases.
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
% | % | % | % | %
0 | 0.27 | 1 | 0.3 | 53
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
% | % | % | % | %
0 | 63 | 94 | 22 | 47
Around 70% of values lie between 0.07% and 0.7% of wasted concrete at Europe level.
The weighted average of 0.27% of wasted concrete in Europe is almost half the average at world level.
The chart pictures 53% of Europe coverage due to missing data.
Around 75% of values lie between 40% and 70% of returned concrete recovered at Europe level.
The chart pictures 47% of Europe coverage due to missing data.
Europe level
Chart: Wasted concrete 53% of GNR pilot sample - Europe (coverage: 20M m3 in 2019)
| 0.12702753367998648 | 0.1347114674185465 | 0.14997139133743734 | 0.18626870714784358 | 0.24420490343842702 | 0.57015700143795967 | 0.57531287873604275 | 0.70339550444005128 | 0.87123195932700259 | 0.89097943170994864 | 0.95300156419484572 | 0.99347274356148574 | 1
 | 0 | 0.00015968 | 0.00042923 | 0.00068792 | 0.00087255 | 0.0017521 | 0.0026083 | 0.0036008 | 0.0046306 | 0.006 | 0.0060854 | 0.0065532 | 0.0099629
Weighted average | 0.0027328 | 0.0027328 | 0.0027328 | 0.0027328 | 0.0027328 | 0.0027328 | 0.0027328 | 0.0027328 | 0.0027328 | 0.0027328 | 0.0027328 | 0.0027328 | 0.0027328 | 0.0027328 | 0.0027328
Chart: Returned Concrete Recovered 46% of GNR pilot sample - Europe (coverage: 18M m3 in 2019)
| 7.4770473186052061E-3 | 0.15419716810767958 | 0.20055736952072623 | 0.39281595883736353 | 0.41029637718688899 | 0.41909841165534301 | 0.46067740436219928 | 0.46658352110356394 | 0.53763058716550893 | 0.56025154389074316 | 0.93363342083993617 | 1
 | 0 | 0.39855 | 0.44328 | 0.50582 | 0.51864 | 0.65278 | 0.66 | 0.6836 | 0.7 | 0.7 | 0.74367 | 0.93526
Weighted average | 0.62787 | 0.62787 | 0.62787 | 0.62787 | 0.62787 | 0.62787 | 0.62787 | 0.62787 | 0.62787 | 0.62787 | 0.62787 | 0.62787 | 0.62787 | 0.62787

## Slide 27: Wasted and returned concrete are not consistently monitored Procedures for returned and scrap concrete are in place in 70% of cases.
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
% | % | % | % | %
0 | 1.08 | 4 | 1 | 44
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
% | % | % | % | %
0 | 18 | 55 | 18 | 20 - 50
Around 70% of values lie between 0.2% and 2% of wasted concrete in North America.
The weighted average of 1% of wasted concrete in North America is twice the average at world level.
The chart pictures 44% of coverage in North America due to missing data.
Around 70% of values lie between 0% and 20% of returned concrete recovered in North America.
The chart pictures 20-50% of coverage in North America due to missing data.
Note: Coverage is not provided for confidentiality reasons.
North America
Chart: Wasted concrete 44% of GNR pilot sample - North America (coverage: 11M m3 in 2019)
| 6.152321216589781E-2 | 0.46365405028767864 | 0.68716624479426713 | 0.88393884595559458 | 0.93647702850168468 | 1
 | 0.002428 | 0.0024822 | 0.01 | 0.019345 | 0.021485 | 0.04
Weighted average | 0.010831 | 0.010831 | 0.010831 | 0.010831 | 0.010831 | 0.010831 | 0.010831 | 0.010831
Chart: Returned Concrete Recovered 20-50% of GNR pilot sample - North America (coverage: 5M-20M m3 in 2019)
| 0.47273688874196934 | 0.53449971467444557 | 0.60682515989660668 | 0.68150148178730485 | 0.9128233761666158 | 1
 | 0 | 0.17331 | 0.18436 | 0.2 | 0.40559 | 0.55219
Weighted average | 0.18096 | 0.18096 | 0.18096 | 0.18096 | 0.18096 | 0.18096 | 0.18096 | 0.18096

## Slide 28: Local Environment Factors
4

## Slide 29: Water withdrawal per unit of concrete varies across regions Water KPIs find heterogeneity, as reported data is scattered around the mean
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
litres/m3 | litres/m3 | litres/m3 | litres/m3 | %
96 | 220 | 477 | 66 | 99
Observations and comments
Water KPIs show that on the sample average:
90% of process water is collected and re-used;
55% of stormwater is collected;
96% of discharged water is treated.
The weighted average of water withdrawal in relation to concrete production in 2019 is of 220 litres/m3 at world level.
The chart pictures 99% of the world coverage. The remaining percentage corresponds to Morocco, where water consumption is not measured. The data collection process highlighted the opportunity to estimate this KPI in the country concerned.
Around 80% of values lie between 100 litres/m3 and 250 litres/m3.
The lowest water withdrawal figures are mainly found in European reporting region, while the highest figures are reported in North America, Asia and Oceania.
World level
Chart: Water withdrawal per unit 100% of GNR pilot sample - World (coverage: 75M m3 in 2019)
| 1.7661765511307187E-3 | 1.9653668240695245E-3 | 3.5719428164195724E-3 | 1.1521899916682265E-2 | 9.9719591810901481E-2 | 0.11024619813302231 | 0.13799601019669955 | 0.13939111236101012 | 0.18480511039196798 | 0.19462661329402317 | 0.19875571716047377 | 0.21443237278355617 | 0.24880409594886024 | 0.25429486300717352 | 0.26535448093257391 | 0.27584586806649325 | 0.31480992370481453 | 0.32455460295977329 | 0.32989796934891419 | 0.35125245744697875 | 0.35905325344986849 | 0.37006387429627152 | 0.38101476134464918 | 0.38169331504794995 | 0.38980084654125274 | 0.43726629893821584 | 0.45404854689764829 | 0.46098483453958095 | 0.5076748956848407 | 0.56738272116790045 | 0.58505378948514097 | 0.61971100454273798 | 0.62179016042045254 | 0.65100668155288621 | 0.70993548834066023 | 0.7232635083081419 | 0.75645028693289784 | 0.89447677699793759 | 0.90077741274180512 | 0.92665700875380852 | 0.93608881088592488 | 0.94522369154396146 | 0.99214177241750834 | 0.99498585001906226 | 0.99882383847691381 | 1
 | 95.5627 | 103.4736 | 113.9079 | 115.9246 | 128.5426 | 133.8662 | 144.7321 | 154.2203 | 154.3039 | 160.16 | 166.4337 | 166.8262 | 170 | 175 | 175.651 | 179.2633 | 182.5996 | 184.6825 | 185.1312 | 186.6181 | 189.8335 | 190.2992 | 191.2649 | 201.8448 | 202.4911 | 202.7555 | 210.0323 | 211.5153 | 219.6716 | 220.8817 | 221.6486 | 240.637 | 247.6583 | 251 | 253 | 264.1291 | 267.7271 | 272.3796 | 278.1146 | 279.6072 | 311.1663 | 329.5776 | 343 | 353.8658 | 401.3841 | 477.1336
Weighted average | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308 | 219.3308

## Slide 30: Water withdrawal per unit of concrete varies across regions Water KPIs find heterogeneity, as reported data is scattered around the mean
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
litres/m3 | litres/m3 | litres/m3 | litres/m3 | %
96 | 180 | 280 | 44 | 100
Observations and comments
Water KPIs show that on the sample average:
96% of process water is collected and re-used;
60% of stormwater is collected;
95% of discharged water is treated.
The weighted average of water withdrawal in relation to concrete production in 2019 is of 180 litres/m3 at Europe level.
The chart pictures 100% of Europe coverage.
Around 80% of values lie between 100 litres/m3 and 210 litres/m3.
The lowest water withdrawal figures are mainly found in central and Eastern Europe.
Europe level
Chart: Water withdrawal per unit 100% of GNR pilot sample - Europe (coverage: 38M m3 in 2019)
| 3.4856469264462871E-3 | 3.8787599265043193E-3 | 7.0494263393565378E-3 | 2.2739105558667812E-2 | 0.19680211951609211 | 0.21757695822013901 | 0.27234274427210192 | 0.27509605541078425 | 0.36472308763069627 | 0.38410636580960478 | 0.39225538023959294 | 0.42319412555051394 | 0.49102861872793896 | 0.51173395041977476 | 0.53096561289004496 | 0.54151104144262174 | 0.58365530259091936 | 0.60526748273089492 | 0.60660664592430547 | 0.62260730690726618 | 0.71628299757020475 | 0.7494036903917719 | 0.84154910361355495 | 0.876423932479094 | 0.94482185966670285 | 0.94892518857236552 | 1
 | 95.5627 | 103.4736 | 113.9079 | 115.9246 | 128.5426 | 133.8662 | 144.7321 | 154.2203 | 154.3039 | 160.16 | 166.4337 | 166.8262 | 170 | 179.2633 | 184.6825 | 185.1312 | 186.6181 | 191.2649 | 201.8448 | 202.4911 | 202.7555 | 210.0323 | 219.6716 | 221.6486 | 240.637 | 247.6583 | 279.6072
Weighted average | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462 | 181.4462

## Slide 31: Water withdrawal per unit of concrete varies across regions Water KPIs find heterogeneity, as reported data is scattered around the mean
Minimum | Weighted average | Maximum | Standard Deviation | Coverage for pilot
litres/m3 | litres/m3 | litres/m3 | litres/m3 | %
182 | 250 | 330 | 50 | 100
Observations and comments
Water KPIs show that on the sample average:
77% of process water is collected and re-used;
42% of stormwater is collected;
97% of discharged water is treated.
The weighted average of water withdrawal in relation to concrete production in 2019 is of 250 litres/m3 in North America.
The chart pictures 100% of coverage in North America.
Around 80% of values lie between 182 litres/m3 and 300 litres/m3.
High water consumption can be caused by the low efficiency of recycling systems due to the layout of plants.
North America
Chart: Water withdrawal per unit 100% of GNR pilot sample - North America (coverage: 25M m3 in 2019)
| 0.11579910308071084 | 0.13898265432176296 | 0.17170563445017817 | 0.34915411933114843 | 0.43598406777591503 | 0.53461341053625233 | 0.94482080525084633 | 0.9728516200477445 | 1
 | 182.5996 | 189.8335 | 190.2992 | 220.8817 | 251 | 267.7271 | 272.3796 | 311.1663 | 329.5776
Weighted average | 248.8554 | 248.8554 | 248.8554 | 248.8554 | 248.8554 | 248.8554 | 248.8554 | 248.8554 | 248.8554 | 248.8554 | 248.8554

## Slide 32: Dust and Noise KPIs find similarities in most reporting sites Dust collection system and Noise Management Plan are dependent on regulatory obligations
Dust KPIs
Almost 100% of sites in the pilot project at world level have a dust collection system in place at silo. The mandatory aspect of dust collection systems at silo explains their implementation in almost all reporting sites.
Around 60% of concrete is produced with dust collection systems at loadpoint in place at world level (53% in Europe, 88% in North America, 60% in South America and 90% in Asia, Oceania and Africa). However, the existence of dust collection system at loadpoint is not relevant for at least 28% of sites at world level. Indeed, dust collection systems at loadpoint depend on the type of plant, with wet or dry batch for example.
Therefore, answers to Dust KPI at loadpoint depends if dust collection device is in place at relevant dust-emitting points in the process. This question may need to be rephrased in the future. Regardless of sites where dust collection systems at loadpoint are not relevant, 85% of sites at world level are equipped with such dust collection systems.
Around 65% of concrete is produced at concrete mixing sites with Fugitive Dust Management Plan in place at world level (52% in Europe, 72% in North America, 68% in South America and 94% in Asia, Oceania and Africa).
Noise KPIs
On average, 80% of concrete is produced with Noise Management Plans in place at world level (83% in Europe, 70% in North America, 88% in South America and 90% in Asia, Oceania and Africa).
Similarly to dust collection system at silo, there are legal requirements of noise limits, which can explain the high number of cases in which Noise Management Plans are implemented.
World level

## Slide 33: Outcomes of the concrete pilot project
5

## Slide 34: The outcomes of the data collection are positive The concrete pilot project highlights the possibility to extend the GNR platform
Conclusions
Beyond the timing constraints participants had to collect data during the crisis of COVID-19, the pilot project allowed to highlight several important elements of the reported data, which appear as:
Available in general: Overall the availability of KPIs was higher than 80% for the pilot participants.
        Around 10 KPIs were available by 100% of pilot participants: Process Water Collected and Re-used, Stormwater Collection, Treatment of Discharged Water, Dust KPIs, Noise KPIs, Procedures for Returned and Scrap Concrete, Average Distribution Distance, Average Concrete Volume Transported and Concrete Production.
        KPIs not corresponding to internal questionnaires were pointed out, like Wasted or Returned Concrete Recovered.
Coherent: In most of the cases, values showed coherence. The discrepancies between figures were verified with standard deviation and found reasonable, according to multiple factors which would explain differences in regions. All contributors contacted for data verification took part and directly redirected questions to reporting countries concerned.
Comprehensible: Most of the KPIs were understood and reported. In each case of missing data, explanatory reasons were given by contributors, who brought methodological clarifications when needed, like in the case of Dust collection system at loadpoint or average distribution distance.
Some recommendations for improvements are provided in the report ‘Feedbacks on GCCA Survey for GNR Concrete Pilot Project’ regarding rewording, clarification and change of units.

## Slide 35: Annexes
6

## Slide 36: Synthesis table : Results by regions (1/2)
Production data |  |  |  |  |  |  | 
# | KPI | Unit | World - Total | Europe – Total | North America - Total | South America - Total | Asia, Oceania, Africa - Total
1 | Concrete production | m3 | 75 299 862 | 38 154 424 | 25 307 828 | 2 613 546 | 9 195 012
2 | Total concrete returned | m3 | 1 391 463 | 157 255 | 164 402 | 1 020 180 | 49 626
3 | Returned concrete recovered | m3 | 185 996 | 101 186 | 41 565 | 13 034 | 30 211
4 | Wasted concrete | m3 | 206 520 | 55 203 | 122 836 | 9 065 | 19 415
5 | Total Electricity Energy for Production | kWh | 247 781 417 | 72 931 858 | 139 540 365 | 8 074 878 | 27 241 276
6 | Total non-Electricity Energy for Production | MJ | 991 734 953 | 46 170 652 | 888 051 319 | N/A | 57 512 982
 | Energy & Climate Change |  |  |  |  |  | 
# | KPI - Process Energy | Unit | World - Average | Europe - Average | North America - Average | South America - Average | Asia, Oceania, Africa - Average
1 | Total Electricity Energy for Production | kWh/m3 | 4 | 3.6 | 5.2 | 3 | 3
2 | Total non-Electricity Energy for Production | MJ/m3 | 29 | 5.7 | 60.3 | 0 | 6
3 | Total non-Electricity Energy for Production | kWh/m3 | 8 | 1.5 | 16.7 | 0 | 2
4 | Total Energy for Production | kWh/m3 | 10 | 4.4 | 21.4 | 3 | 5
# | KPI - Concrete Transport | Unit | World - Average | Europe - Average | North America - Average | South America - Average | Asia, Oceania, Africa - Average
1 | Type of fuel |  | Diesel | Diesel | Diesel | Diesel | Diesel
2 | Average distribution distance | km | 16 | 12 | 23 | 20 | 20
3 | Average concrete volume transported | m3 / delivery | 6.6 | 7 | 6.4 | 7 | 6
4 | Average fuel consumption | km/l or 1000 m3 | 1.15 | 1.4 | 0.8 | 1 | 2
5 | Fuel consumption by km by m3 | l/km/m3 | 4.8 | 3.3 | 7.5 | 7 | 3
6 | CO2 from transport | kg CO2 / m3 | 11 | 9 | 13 | 33 | 8

## Slide 37: Synthesis table : Results by regions (2/2)
KPIs at Country level |  |  |  |  |  |  |  | 
Local environment factors (water, dust and noise) |  |  |  |  |  |  |  | 
# | Water KPIs |  | Unit | World - Average | Europe - Average | North America - Average | South America - Average | Asia, Oceania, Africa - Average
1 | Process Water Collected and Re-used |  | Y/N | 90% | 96% | 77% | 100% | 100%
2 | Stormwater Collection |  | Y/N | 55% | 60% | 42% | 95% | 53%
3 | Water Withdrawal |  | Litres | 904 270 950 | 507 973 361 | 1 535 197 664 | 179 995 470 | 1 065 180 773
4 | Water Withdrawal Per Unit |  | Litres/m3 concrete | 220 | 180 | 250 | 253 | 292
5 | Treatment of Discharged Water |  | Y/N | 96% | 95% | 97% | 97% | 94%
# | Dust KPI |  | Unit | World - Average | Europe – Average | North America - Average | South America - Average | Asia, Oceania, Africa - Average
1 | Dust Collection: Silo |  | Y/N | 99.89% | 100% | 99.87% | 98% | 100%
2 | Dust Collection: Loadpoint |  | Y/N | 87% | 96% | 80% | 61% | 90%
3 | Fugitive Dust Management Plan |  | Y/N | 64% | 52% | 72% | 68% | 94%
# | Noise KPI |  | Unit | World - Average | Europe - Average | North America - Average | South America - Average | Asia, Oceania, Africa - Average
1 | Noise Management Plan |  | Y/N | 79% | 83% | 69% | 88% | 90%
Circular Economy |  |  |  |  |  |  |  | 
# | KPI |  | Unit | World - Average | Europe - Average | North America - Average | South America - Average | Asia, Oceania, Africa - Average
1 | Procedures for Returned and Scrap Concrete |  | Y/N | 70% | 69% | 63% | 52% | 94%
2 | Returned Concrete Recovered |  | % | 53% | 63% | 18% | 26% | 80%
3 | Wasted Concrete |  | % | 0.5% | 0.27% | 1.08% | 1% | 0.22%
4 | Alternative aggregates used (test) |  | ton | 300 | N/A | N/A | N/A | 300